BLACKFRIAR PAINTS LTD.

Revision Date:

15/03/2011

TECHNICAL DATA  SHEET
AE022 Blackfriar Line Marking Paint Aerosol.

| ## Product Information # Description # A quick drying line marking paint supplied ready for use in handy 750ml aerosol pack. Usage/purpose Ideal for marking factory floors, car parks step edges and general delineation. Characteristics Quick drying with good light and colour fastness. Finish Semi Gloss ### Colour(s) White, Yellow, Red, Blue, Green & Black Packaging 750ml Aerosol Disclaimer; The information contained herein is to the best of our knowledge true and accurate and is given in good faith but without warranty. It is our recommendation that a trial area is first coated to ensure the product is satisfactory to individual requirements. | ### Technical Spec Composition Based on a high quality blend of alkyd resins coupled with carefully selected pigments and extenders to give good light fastness and durability. ### VOC 570 g/litre ### Performance Interior or exterior Use. Surface Preparation Ensure the substrate to be painted is sound and free from any surface contaminant likely to give adhesion problems (e.g. wax, grease etc). ##### Application ##### Method Supplied ready for use. Aerosol can will also fit most linemarking machines ### For Technical Enquiries Material Safety Data Sheets. Contact Sales on 0191 4106611 | Recommended Spreading Rate One can covers approximately 6-8m2 ### Drying Time Dry in 10-20 mins under normal conditions (20°C 50% RH). ### Cleaning Use xylene or paint thinners Limitations Avoid application in damp, wet or very windy conditions. Environmental Info. Over 75% of local authorities collect aerosols in their can banks along with drinks cans or through their kerbside collection schemes. To find out if your local authority is amongst them, contact your local recycling officer |
| --- | --- | --- |
|  |  | Paint Product UN No. 1950. |
|  |  | Tor Coatings Ltd. Portobello Industrial Est, Birtley Chester-le Street County Durham DH3 2RE |