BLACKFRIAR PAINTS LTD
TECHNICAL DATA  SHEET
BF058 & 59 BLACKFRIAR LINE MARKING PAINT

Revision date: 20/06/11

| ## Product Information # Description # A quick drying line marking paint. Usage/purpose Ideal for marking factory floors, car parks, step edges etc. Characteristics Quick Drying. Finish Semi-Gloss ### Colour(s) White, Yellow. Packaging 1 litre, 2.5 litre, 5 litre. Larger sizes may be available on request dependant on volume required Disclaimer; The information contained herein is to the best of our knowledge true and accurate and is given in good faith but without warranty. It is our recommendation that a trial area is first coated to ensure the product is satisfactory to individual requirements | ### Technical Spec Composition A blend of lightfast pigments in a binding resin. ### Properties EU limit value for this product (cat A/i): 500 g/l. This product contains max 500 g/l VOC ### Performance Interior or exterior use. Surface Preparation Ensure the substrate to be painted is sound and free from any surface contaminant likely to give adhesion problems (e.g. wax, grease etc). It is essential that the surface is thoroughly dry prior to application material. ##### Application ##### Method #### Brush, Roller, Spray ##### Ensure products are thoroughly stirred with a broad stirrer. Two coats are recommended ### For Technical Enquiries, Material Safety Data Sheets ###### Telephone 0191 4106611 | Recommended Spreading Rate 13m²/ltr (approx.) ### Thinning Up to 10% with Blackfriar Line Marking Thinners. ### Drying Time Dry in 30 minutes under normal conditions (20°C 50% R/H). ### Cleaning Clean application equipment or spills immediately Blackfriar Line Marking Thinners Only. Do not use White Spirit. Limitations Not suitable for use as a floor paint (solely for line marking). Do not apply in damp, wet or very hot conditions. Environmental Info. Highly flammable |
| --- | --- | --- |
|  |  | Paint Product UN No. 1263. |
|  |  | Tor Coatings Ltd. Portobello Industrial Est, Birtley Chester-le Street County Durham DH3 2RE |