BF2060013 SOLAR REFLECTIVE PAINT ALUMINIUM

SOLAR REFLECTIVE ALUMINIUM PAINT

EXTERIOR USE BITUMEN BASED FIBRE REINFORCED CONTAINS REFLECTIVE ALUMINIUM

BLACKFRIAR PROFESSIONAL SOLAR REFLECTIVE PAINT ALUMINIUM Blackfriar Professional Solar Reflective Paint Aluminium is a blend of rubber, polymer modified bitumen, aluminium and fibre reinforcement. For the refurbishment or repair of porous asbestos, corrugated iron, concrete, tiled and felted roofs.

PREPARATION Surfaces should preferably be as dry as possible. Emergency patch repairs can however be successfully completed to surfaces with running water. Remove any loose material and dirt. Very porous, dry surfaces should be primed with Blackfriar Professional Solar Reflective Paint Aluminium diluted with 25% white spirit. A wire brush should be used to remove all traces of moss etc. A fungicide like Blackfriar Anti-Mould Solution or Concentrated Fungicidal Wash may be required for heavily contaminated surfaces. Specialist advice must be sought when dealing with old asbestos/cement roofs.

APPLICATION Blackfriar Professional Solar Reflective Paint Aluminium should be applied generously by brush at the rate of 1m2/L per coat. If a second coat is required it should be applied at right angles to the first coat. Do not brush out to a thin film. Cracks, splits, holes and leaks around roof sheet overlaps should be treated in the following manner. Apply a generous coat of Blackfriar Professional Solar Reflective Paint Aluminium and immediately bed in a strip of scrim cut to a suitable size. Apply a further coat of Blackfriar Professional Solar Reflective Paint Aluminium over the scrim using a stippling action and leave to cure. Deep pits and cracks in flat concrete roofs should be filled prior to coating. Blackfriar Professional Solar Reflective Paint Aluminium is not suitable for coating bare wooden substrates in order to form a waterproofing seal. Entrapped moisture on porous surfaces may cause blistering in warm weather or spalling at low temperatures. Only limited emergency patch repairs should therefore be made to porous surfaces while wet. Not suitable for use on EPDM rubber roofs. Check compatibility with other surfaces if in doubt.

APPEARANCE Textured Finish Aluminium

COVERAGE RATE Typically 1m2/L per coat. Two coats recommended. Roof overlaps and cracks, splits and holes will require a heavier application ideally with the use of scrim.

DRYING TIME 16-24hrs @20°C. Allow to dry for a minimum of 24hrs @20°C between coats. Full cure is achieved in 5-7 days @20°C. Note curing will only commence once any surface water has evaporated.

Pack Sizes 5L

CLEAN UP Remove as much product from application equipment as possible before washing with White Spirits. Do not empty into drains or watercourses. Some local authorities have special facilities for the disposal of waste coatings.

VOC EU limit value for this product (cat A/i): 500 g/l. This product contains max 500 g/l VOC

DISCLAIMER The information contained herein is to the best of our knowledge true and accurate and is given in good faith but without warranty. It is our recommendation that a trial area is first coated to ensure the product is satisfactory to individual requirements.

Tor Coatings Ltd, Portobello Industrial Estate, Birtley, Chester-le-Street, County Durham, DH3 2RE. For Technical Enquiries or Material Safety Data Sheets. Contact sales on 0191 410 6611.