BF2070008 WATER BASED FLOOR SEALER

SEALS POROUS SUBSTRATES

INTERIOR AND EXTERIOR USE SEALS POROUS SUBSTRATES BINDS AND STABILISES FRIABLE SUBSTRATES

BLACKFRIAR PROFESSIONAL WATER BASED FLOOR SEALER Blackfriar Professional Water Based Floor Sealer is a single pack low odour sealer. Ideal for binding, stabilizing and sealing friable and porous substrates prior to finishing with water based coatings like Blackfriar Professional Acrylic Floor Paint. Also suitable to apply under water based masonry paints.

PREPARATION Ensure the surface to be painted is sound, clean, dry and free from grease or any substance liable to give adhesion problems. Scrape off any old or flaking paint until you have a firm surface. Special attention should be given to areas under cars to ensure all oil, grease, dirt and road salt is removed. New concrete must be left for at least 6 months before applying Blackfriar Professional Water Based Floor Sealer.

APPLICATION Stir thoroughly before use. Apply with a brush or roller working the paint in any surface imperfections. Blackfriar Professional Water Based Floor Sealer is not suitable for use over non porous substrates like PVC, thermoplastic tiles, quarry tiles or granolithic concrete. Do not apply it on concrete surfaces treated with alkali containing liquids, areas subjected to rising damp or areas treated with PVA bonding solutions. Do not apply in cold (below 10°C), damp or humid conditions. If concrete floors are very smooth then pre-treat with Blackfriar Professional Acid Etch followed after thorough rinsing by Blackfriar Professional Water Based Floor Sealer.

APPEARANCE Gloss Finish. Clear

COVERAGE RATE 10-15m2/litre per coat.

DRYING TIME 2-4hrs @20°C. Allow to dry for a minimum of 4hrs @20°C between coats. Full cure is achieved in 3-5 days @20°C. Best results are achieved in warm (15°C), dry conditions with good ventilation. Lower temperatures and higher humidity will prolong the drying times.

PACK SIZES 5L

CLEAN UP Remove as much product from application equipment as possible before washing with water. Do not empty into drains or watercourses.Some local authorities have special facilities for the disposal of waste coatings.

VOC EU limit value for this product (cat A/i): 140 g/l. This product contains max 140 g/l VOC

DISCLAIMER The information contained herein is to the best of our knowledge true and accurate and is given in good faith but without warranty. It is our recommendation that a trial area is first coated to ensure the product is satisfactory to individual requirements.

Tor Coatings Ltd, Portobello Industrial Estate, Birtley, Chester-le-Street, County Durham, DH3 2RE. For Technical Enquiries or Material Safety Data Sheets. Contact sales on 0191 410 6611.